## Slide 1: ME 607 Introduction to composite materials
Term Project:
Complete and partial degradation of laminate under mechanical and hygro-thermal loading
Group no: 1
Sabyasachi Kashyap (244103429)
Dushyant Pratap Singh (244103101)
Vikas Prajapati (244103107)
Partha Pratim Borah (246103104)

## Slide 2: Complete and partial degradation of composites
Complete Degradation
Assumes that once a failure criterion is met, the material properties at the failed point reduce to zero instantly.
Partial Degradation
Only the failed material stiffness components reduced others remains intact.
For e.g.: Uniaxial loading in direction and ply failed (FPF)
Solve for
For e.g.: Based on the failure mode:
Longitudinal: ,
Transverse: ,
Shear:

## Slide 3
Glass epoxy laminate properties:
m/m/
m/m/
m/m/Kg/Kg
m/m/Kg/Kg
Hygrothermal properties:
Mechanical loading:
Fig: Glass epoxy laminate

## Slide 4
Complete Degradation

## Slide 5
Complete degradation of laminate
Ply |  |  |  |  |  |  | Failure mode
 |  |  | 0 | (LC) | (TC) | 0 | TC
 |  |  |  | (LC) | 18.465 (TC) | 17.939 (S) | TC
 |  |  |  | (LC) | 18.465 (TC) | 17.939 (S) | TC
 |  |  | 0 | (LC) | (TC) | 0 | TC
Ply |  |  |  |  |  |  | Failure mode
 |  |  | 0 |  |  | 0 | TC
 |  |  |  |  | 18.465 (TC) | 17.939 (S) | TC
 |  |  |  |  | 18.465 (TC) | 17.939 (S) | TC
 |  |  | 0 |  |  | 0 | TC
Ply layer 4 will fail
Iteration 1

## Slide 6
Complete degradation of laminate
Ply |  |  |  |  |  |  | Failure mode
 |  |  | 0 | 3.051 (LC) | 12.859 (TC) | 0 | TC
 |  |  |  | 5.284 (LC) | 27.318 (TC) | 32.297 (S) | S
 |  |  |  | 5.284 (LC) | 27.318 (TC) | 32.297 (S) | S
 | Fully Degraded |  |  |  |  |  | 
Ply |  |  |  |  |  |  | Failure mode
 |  |  | 0 | 3.051 (LC) | 12.859 (TC) | 0 | TC
 |  |  |  | 5.284 (LC) | 27.318 (TC) | 32.297 (S) | S
 |  |  |  | 5.284 (LC) | 27.318 (TC) | 32.297 (S) | S
 | Fully Degraded |  |  |  |  |  | 
Ply layer 2 & layer 3 will fail
Iteration 2

## Slide 7
Complete degradation of laminate
Ply |  |  |  |  |  |  | Failure mode
 |  |  | 0 | 1.098 (LC) | 21.42 (TC) | 0 | TC
 | Fully Degraded ( Iteration) |  |  |  |  |  | 
 | Fully Degraded ( Iteration) |  |  |  |  |  | 
Ply |  |  |  |  |  |  | Failure mode
 |  |  | 0 | 1.098 (LC) | 21.42 (TC) | 0 | TC
Ply layer 1 will fail
Iteration 3

## Slide 8
Partial Degradation

## Slide 9
Partial degradation of laminate
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 0 | (LC) | (TC) | 0 | TC
2 |  |  |  |  | (LC) | 18.465 (TC) | 17.939 (S) | TC
3 |  |  |  |  | (LC) | 18.465 (TC) | 17.939 (S) | TC
4 |  |  |  | 0 | (LC) | (TC) | 0 | TC
5 |  |  |  | 0 | (LC) | (TC) | 0 | TC
6 |  |  |  |  | (LC) | 18.465 (TC) | 17.939 (S) | TC
7 |  |  |  |  | (LC) | 18.465 (TC) | 17.939 (S) | TC
8 |  |  |  | 0 | (LC) | (TC) | 0 | TC
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 0 |  |  | 0 | TC
2 |  |  |  |  |  | 18.465 (TC) | 17.939 (S) | TC
3 |  |  |  |  |  | 18.465 (TC) | 17.939 (S) | TC
4 |  |  |  | 0 |  |  | 0 | TC
5 |  |  |  | 0 |  |  | 0 | TC
6 |  |  |  |  |  | 18.465 (TC) | 17.939 (S) | TC
7 |  |  |  |  |  | 18.465 (TC) | 17.939 (S) | TC
8 |  |  |  | 0 |  |  | 0 | TC
Iteration 1

## Slide 10
Ply layer 4 and 5 will fail
Iteration 1: cont…

## Slide 11
Partial degradation of laminate
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 0 | 4.248 (LC) | 7.123 (TC) | 0 | TC
2 |  |  |  |  | 3.243 (LC) | 16.762 (TC) | 17.267 (S) | S
3 |  |  |  |  | 3.243 (LC) | 16.762 (TC) | 17.267 (S) | S
4 |  |  |  | 0 | 0 |  |  | 
5 |  |  |  | 0 | 0 |  |  | 
6 |  |  |  |  | 3.243 (LC) | 16.762 (TC) | 17.267 (S) | S
7 |  |  |  |  | 3.243 (LC) | 16.762 (TC) | 17.267 (S) | S
8 |  |  |  | 0 | 4.248 (LC) | 7.123 (TC) | 0 | TC
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 0 | 4.248 (LC) | 7.123 (TC) | 0 | TC
2 |  |  |  |  | 3.243 (LC) | 16.762 (TC) | 17.267 (S) | S
3 |  |  |  |  | 3.243 (LC) | 16.762 (TC) | 17.267 (S) | S
4 |  |  |  | 0 | 0 |  |  | 
5 |  |  |  | 0 | 0 |  |  | 
6 |  |  |  |  | 3.243 (LC) | 16.762 (TC) | 17.267 (S) | S
7 |  |  |  |  | 3.243 (LC) | 16.762 (TC) | 17.267 (S) | S
8 |  |  |  | 0 | 4.248 (LC) | 7.123 (TC) | 0 | TC
Iteration 2

## Slide 12
Ply layer 2 & 7 and ply layer 3 & 6 will fail
Iteration 2: cont…

## Slide 13
Partial degradation of laminate
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 0 | 3.956 (LC) | 7.349 (TC) | 0 | TC
2 |  |  |  |  | 3.292 (LC) | 17.02 (TC) |  | 
3 |  |  |  |  | 3.292 (LC) | 17.02 (TC) |  | 
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 3.292 (LC) | 17.02 (TC) |  | 
7 |  |  |  |  | 3.292 (LC) | 17.02 (TC) |  | 
8 |  |  |  | 0 | 3.956 (LC) | 7.349 (TC) | 0 | TC
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 0 | 3.956 (LC) | 7.349 (TC) | 0 | TC
2 |  |  |  |  | 3.292 (LC) | 17.02 (TC) |  | 
3 |  |  |  |  | 3.292 (LC) | 17.02 (TC) |  | 
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 3.292 (LC) | 17.02 (TC) |  | 
7 |  |  |  |  | 3.292 (LC) | 17.02 (TC) |  | 
8 |  |  |  | 0 | 3.956 (LC) | 7.349 (TC) | 0 | TC
Iteration 3

## Slide 14
Ply layer 2 & 7 and ply layer 3 & 6 will fail
Iteration 3: cont…

## Slide 15
Partial degradation of laminate
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 0 | 2.52 (LC) | 5.69 (TC) | 0 | TC
2 |  |  |  |  | 1.963 (LC) |  |  | 
3 |  |  |  |  | 1.963 (LC) |  |  | 
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 1.963 (LC) |  |  | 
7 |  |  |  |  | 1.963 (LC) |  |  | 
8 |  |  |  | 0 | 2.52 (LC) | 5.69 (TC) | 0 | TC
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 0 | 2.52 (LC) | 5.69 (TC) | 0 | TC
2 |  |  |  |  | 1.963 (LC) |  |  | 
3 |  |  |  |  | 1.963 (LC) |  |  | 
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 1.963 (LC) |  |  | 
7 |  |  |  |  | 1.963 (LC) |  |  | 
8 |  |  |  | 0 | 2.52 (LC) | 5.69 (TC) | 0 | TC
Iteration 4

## Slide 16
Ply layer 8 will fail
Iteration 4: cont…

## Slide 17
Partial degradation of laminate
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 60.48 | 2.32 (LC) | 11 (TC) | 0.84 (S) | TC
2 |  | 1874.1 |  |  | 3.072 (LC) |  |  | 
3 |  |  |  |  | 2.425 (LC) |  |  | 
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 0.484 (LC) |  |  | 
7 |  |  |  |  | 0.0935 (TC) |  |  | 
8 |  |  |  | 0 | 2.914 (LC) |  |  | 
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  |  | 60.48 | 2.32 (LC) | 11 (TC) | 0.84 (S) | TC
2 |  |  |  |  | 3.072 (LC) |  |  | 
3 |  |  |  |  | 2.425 (LC) |  |  | 
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 0.484 (LC) |  |  | 
7 |  |  |  |  | 0.0935 (TC) |  |  | 
8 |  |  |  | 0 | 2.914 (LC) |  |  | 
Iteration 5

## Slide 18
Ply layer 1 will fail
Iteration 5: cont…

## Slide 19
Partial degradation of laminate
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  | 0 | 0 | 2.4 (LC) |  |  | LC
2 |  |  |  |  | 1.202 (LC) |  |  | LC
3 |  |  |  |  | 1.202 (LC) |  |  | LC
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 1.202 (LC) |  |  | LC
7 |  |  |  |  | 1.202 (LC) |  |  | LC
8 |  |  | 0 | 0 | 2.4 (LC) |  |  | LC
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  | 0 | 0 | 2.4 (LC) |  |  | LC
2 |  |  |  |  | 1.202 (LC) |  |  | LC
3 |  |  |  |  | 1.202 (LC) |  |  | LC
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 1.202 (LC) |  |  | LC
7 |  |  |  |  | 1.202 (LC) |  |  | LC
8 |  |  | 0 | 0 | 2.4 (LC) |  |  | LC
Iteration 6

## Slide 20
Ply layer 1 and 8 both will fail
Iteration 6: cont…

## Slide 21
Partial degradation of laminate
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  | 0 | 0 |  |  |  | 
2 |  |  |  |  | 1.202 (LC) |  |  | LC
3 |  |  |  |  | 1.202 (LC) |  |  | LC
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 1.202 (LC) |  |  | LC
7 |  |  |  |  | 1.202 (LC) |  |  | LC
8 |  | 0 | 0 | 0 |  |  |  | 
Ply |  |  |  |  |  |  |  | Failure mode
1 |  |  | 0 | 0 |  |  |  | 
2 |  |  |  |  | 1.202 (LC) |  |  | LC
3 |  |  |  |  | 1.202 (LC) |  |  | LC
4 |  | 0 |  | 0 | 0 |  |  | 
5 |  | 0 |  | 0 | 0 |  |  | 
6 |  |  |  |  | 1.202 (LC) |  |  | LC
7 |  |  |  |  | 1.202 (LC) |  |  | LC
8 |  | 0 | 0 | 0 |  |  |  | 
Iteration 7

## Slide 22
Ply layer 1 and 8 both will fail
Iteration 7: cont…

## Slide 23
Thank you